Tony’s Acrylic Finishing Process
1. Turn pen to size

2. In reverse direction, and at 500 to 700 rpms, sand from 320 to 600, or 150 to 600 if necessary. I have done this wet and dry, but prefer dry to make it easier to see the white sanding powder on the blank. Don’t move on to next grit until the blank is completely covered with white powder.

3. Before starting the next higher grit, sand longitudinally with the lathe off. Simply rotate the lathe a little at a time as you sand lengthwise. Blot white sanding power with a damp paper towel – lathe should not be rotating when sanding lengthwise.

4. After sanding, move on to your MM (wet only). I change the direction of the lathe to forward and set at 1300 to 1500 rpms.  So far I have not had to go beyond 1500 to 4000 (Teal) grit with the MM (but goes as high as you like). I also continue to clean with damp paper towels.

5. Make sure blank is dry, and apply a two or three drops of Meguiars 105 auto polish. DO NOT LET IT DRY TO A HAZE. Turn on lathe (forward at 1300 to 1500 rpms) and run a micro fiber, terry cloth, or cotton t-shirt to “rub –in” and remove the 105 product. I do that for about 7 to 10 seconds. I repeat this process again.
6. Next do the same as above (and do it twice) with Meguiars 205 auto polish. 

7. Examine polished blank under bright like. You should be 99 to 100% scratch-free.

8. Lastly, apply a thin coating of Rejex. THIS MUST DRY TO A HAZE, and it takes about 15 minutes. Wipe-of using any of the aforementioned cloths and enjoy!

The blanks will be incredibly slick, so handle carefully.

